TEMPLATE:
Material Name:
Material Type:
Manufacturer:
SDS Link: Unavailable
REPORT Link: Unavailable
Material Basic Info
- Bed Adhesion Needs:
- Print Temp Range:
- Bed Temp Range:
- Speeds:
- Fan/Cooling:
- Retraction:
- Layer Height Range:

Drying Info:
Annealing info:
NOTES:

___________________________________________________________________________________

Material Data Bellow
IN PROGRESS!

Material Name: PLA
Material Type: Polylactic Acid
Manufacturer: Polymaker
SDS Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/SDS/PolyLite_PLA_MSDS.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/REPORTS/filament_testing_polylite_PLA.odt
Material Basic Info
- Print Temp Range: 190-230 C
- Bed Temp Range: 25-60 C
- Speeds: 40-60mm/s
- Fan/Cooling: ON - 100%
- Retraction: --
- Layer Height Range:
Drying Notes: 80 C for 8 hours.
NOTES:
DUAL MATERIAL COMPATIBILITY:
PLA(model) + Ninjaflex(model) = Does not stick well
PLA(model) + Ninjaflex(support) = Not advisable, ninjaflex is a bad support material
PLA(support) + Ninjaflex(model) = MATCH (works great!)
___________________________________________________________________________________

Material Name: ABS
Material Type: Acrylonitrile-Butadiene-Styrene Copolymer
Manufacturer: IC3D
SDS Link: /home/aleph/shared-j/devel/lulzbot/filament/ic3d/SDS/IC3D PA 747 ABS MSDS.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/ic3d/ic3d_ABS.odt
Material Basic Info
- Print Temp Range: 210 - 255 C (NEVER OVER 260 C!)
- Bed Temp Range: 95 - 110 C
- Speeds: --
- Fan/Cooling: OFF
- Retraction: --
- Layer Height Range: 0.05 - 1.2mm
Drying Info: Once a month for 4 hours at 70 C
NOTES: Best if printed in a warm enclosure.
___________________________________________________________________________________
Material Type: ABS
Manufacturer: Chromastrand Labs
SDS Link: http://devel.alephobjects.com/lulzbot/filament/chromastrand/SDS's/MSDS_CHroma%20Strand_ABS.pdf
REPORT Link: Unavailable
Material Basic Info
- Print Temp Range: 235-245 C
- Bed Temp Range: 95-110 C
- Speeds: 40mm/s
- Fan/Cooling: OFF (if ON, never over 10%)
- Retraction: 1mm @ 10mm/s
- Layer Height Range: 0.05 - 1.2mm
Drying Info: Dry about once a month if left out for 8 hours at 80 C
NOTES: Best if printed inside of a warm enclosure.
DUAL COMPATIBILITY NOTES:
Ninjaflex is a Compatible Material for Chroma ABS.
Polylite PLA is a good Support Material for Chroma ABS. (NOTE: disable cooling fan on the PLA profile)
___________________________________________________________________________________

Material Name: nGen
Material Type: Amphora 3300 (?)
Manufacturer: Colorfabb
SDS Link: http://devel.alephobjects.com/lulzbot/filament/colorfabb/SDSs/Eastman_SDS-Eastman-Amphora(TM)3D-Polymer-AM3300.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/colorfabb/colorfab_n-gen_testing_notes.odt
http://devel.alephobjects.com/lulzbot/filament/colorfabb/colorfab_ngen_flex_testing_notes.odt
Material Basic Info
- Print Temp Range: 220-240C
- Bed Temp Range: 75-85C
- Speeds: 40-60mm/s
- Fan/Cooling: 50%
- Retraction: 1-2mm/10-25s
- Layer Height Range:
Drying Info: 65C (149F) for more than 2 hours (after 2 days of air exposure)
NOTES: https://ngen.colorfabb.com/
___________________________________________________________________________________

Material Name: PolyCast
Material Type:
Manufacturer: Polymaker
SDS Link:
REPORT Link:
Material Basic Info
- Print Temp Range: 120C - 220C
- Bed Temp Range: 25C - 70C
- Speeds: 40 - 60mm/s
- Fan/Cooling: ON
- Retraction: --
- Layer Height Range: --
Drying Info:
60C for 12 hours
___________________________________________________________________________________

Material Name: Polymax PC (formerly PC-Max)
Material Type: Polycarbonates (PC)
Manufacturer: Polymaker
SDS Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/SDS/Polymaker%20PC-Max_MSDS%20v1.1.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/REPORTS/filament_testing_polymaker_pc_max.pdf
Material Basic Info
- Print Temp Range: 250C - 270C
- Bed Temp Range: 90C - 105C
- Speeds: 30mm/s - 50mm/s
- Fan/Cooling: OFF
- Retraction: --
- Layer Height Range: --
Drying Info:
Dry at 80C for 8 hours
NOTES: https://us.polymaker.com/product/polymax-pc/
___________________________________________________________________________________

Material Name: Pa-Cf
Material Type: carbon Fiber Filled Polyamide
Manufacturer: Colorfabb
SDS Link: http://devel.alephobjects.com/lulzbot/filament/colorfabb/PA-CF_Low_Warp/SDS_E%20Colorfabb%20PA-CF%20%20Low%20Warp%20v1.1.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/colorfabb/PA-CF_Low_Warp/NEW-MATERIAL-REPORT_CF_PA-CF.odt
Material Basic Info
- Print Temp Range: 260C - 280C
- Bed Temp Range: 40C- 50C
- Speeds: 30mm/s - 40mm/s
- Fan/Cooling: 50%
- Retraction: --
- Layer Height Range: Minimum of 0.2mm layer height
Drying Info: 70-80C for 4-6 hours
NOTES: https://colorfabb.com/pa-cf-low-warp
___________________________________________________________________________________

Material Name: Polyflex
Material Type:
Manufacturer: Ploymaker
SDS Link:
REPORT Link:
Material Basic Info
- Print Temp Range: 210C - 230C
- Bed Temp Range: 25C - 60C
- Speeds: 20mm/s - 40mm/s
- Fan/Cooling: ON
- Retraction: --
- Layer Height Range: --
Drying Info:
70C for 12 hours
___________________________________________________________________________________

Material Name: Ninjaflex
Material Type: Thermoplastic polyurethane
Manufacturer: Ninjatek
SDS Link: http://devel.alephobjects.com/lulzbot/filament/Ninjaflex/SDS-NinjaFlex.odg
REPORT Link: UNAVAILABLE
Material Basic Info
- Print Temp Range: 225C - 235C
- Bed Temp Range: Room Temp - 60C
- Speeds: Top/bottom 10 - 20mm/s, Infill/Shell 15 - 35mm/s
- Fan/Cooling: On after layer 2
- Retraction: --
- Layer Height Range: --
Drying Info:
135 F for 6 hours
NOTES: https://ninjatek.com/ninjaflex/
DUAL COMPATIBILITY NOTES:
PLA is a good Support Material for Ninjaflex.
PETG is a Compatible Material for Ninjaflex. (NOTE: Turn Cooling DOWN on the NINJAFLEX PROFILE)
Chomrastrand Labs ABS is a Compatible Material for Ninjaflex.
___________________________________________________________________________________

Material Name: PVA
Material Type: Polyvinyl Alcohol
Manufacturer: eSun
SDS Link: http://devel.alephobjects.com/lulzbot/filament/esun/PVA/SDS/msds_esun_pva.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/esun/PVA/PVA_Testing_Notes.odt
Material Basic Info
- Print Temp Range: 190C - 200C
- Bed Temp Range: 45C - 60C
- Speeds: 30mm/s
- Fan/Cooling: 10% - 50%
- Retraction: --
- Layer Height Range: --
Drying Info:
45C (113F) for 10 hours
NOTES: http://www.esun3d.net/products/82.html
___________________________________________________________________________________

Material Name: Alloy 910
Material Type: Polyamide copolymer, Nylon 6/69
Manufacturer: Taulman
SDS Link: http://devel.alephobjects.com/lulzbot/filament/taulman/910/SDS/SDS_Alloy%20910.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/taulman/910/Testing_Docs/nylon910_3mm.odt
Material Basic Info
- Print Temp Range: 250C - 260C
- Bed Temp Range: 45C
- Speeds: 40mm/s
- Fan/Cooling: OFF
- Retraction: 3 - 4mm
- Layer Height Range: --
Drying Info:
120F for 24 hours
NOTES: http://taulman3d.com/910-features.html
___________________________________________________________________________________

Material Name: Bridge Nylon
Material Type: Nylon 6 6,6 6T
Manufacturer: Taulman
SDS Link: http://devel.alephobjects.com/lulzbot/filament/taulman/SDS's/msds_taulman_nylon_bridge.pdf
http://devel.alephobjects.com/lulzbot/filament/taulman/Bridge/SDS/SDS_Nylon%20645-B%20Bridge.pdf
REPORT Link: UNAVAILABLE
Material Basic Info
- Print Temp Range: 250C - 265C
- Bed Temp Range: 45C
- Speeds: 30mm/s - 35mm/s
- Fan/Cooling: OFF
- Retraction: 3 - 4mm
- Layer Height Range: --
Drying Info:
120F for 24 hours
NOTES: http://taulman3d.com/bridge-nylon.html
___________________________________________________________________________________

Material Name: PolyMide™ PA6-CF
Material Type: Polyamide 6 with Carbon Fiber @ <30%
Manufacturer: Polymaker
SDS Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/SDS/N600CF20_SDS_EN_V1.pdf
REPORT Link:
Material Basic Info
- Bed Adhesion Needs: USE GLUE STICK
- Print Temp Range: 250-280 C
- Bed Temp Range: 25-50C (DO NOT EXCEED 50C)
- Speeds: 60 mm/s
- Fan/Cooling: OFF
- Retraction: --
- Layer Height Range: --
Drying Info: 80 C for 12 Hrs
Annealing Info: 90C for 2 Hrs
NOTES: https://us.polymaker.com/product/polymide-pa6-cf/
https://polymaker.com/Downloads/PIS/PolyMide_PA6-CF_PIS_EN_V1.2.pdf
___________________________________________________________________________________

Material Name: PA6-GF
Material Type: Polyamide-amide 6 Glass filled
Manufacturer: Polymaker
SDS Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/SDS/N600GF25_SDS_EN_V1.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/REPORTS/N600GF-TESTING-REPORT.odt
Material Basic Info
*USE GLUE STICK
- Print Temp Range: 250-280 C (up to 300C)
- Bed Temp Range: 25C to 50C (DO NOT EXCEED 50 C)
- Speeds: 60mm/s
- Fan/Cooling: OFF
- Retraction: --
- Layer Height Range: --
Drying Info: 80 C for 12 Hrs
Annealing: (None?)
NOTES: https://us.polymaker.com/product/polymide-pa6-gf/
___________________________________________________________________________________

Material Name: Polydissolve
Material Type:
Manufacturer: Polymaker
SDS Link:
REPORT Link:
Material Basic Info
- Print Temp Range: 215C - 225C
- Bed Temp Range: 25C - 60C
- Speeds: 20 - 40mm/s
- Fan/Cooling: ON
- Retraction: --
- Layer Height Range: --
Drying Info:
80C for 12 hours
NOTES:
___________________________________________________________________________________

Material Name: CoPa
Material Type: Polyamide Copolymer
Manufacturer: Polymaker
SDS Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/PolyMide/PolyMide%e2%84%a2%20CoPA_SDS_V3.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/PolyMide/PolyMide_REPORT-.odt
Material Basic Info
- Print Temp Range: 250C - 270C
- Bed Temp Range: 25C - 70C
- Speeds: 30 - 50mm/s
- Fan/Cooling: OFF
- Retraction: --
- Layer Height Range: --
Drying Info:
80C for 12 hours
Annealing Info:
70C for 2 hours
NOTES: https://us.polymaker.com/product/polymide-copa/
___________________________________________________________________________________
Material Name: N600
Material Type: Polyamide 6
Manufacturer: Polymaker
SDS Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/SDS/N600_SDS_EN_V1.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/polymaker/REPORTS/Polymaker_N600_NEW-MATERIAL-TESTING-REPORT.odt
Material Basic Info
- Print Temp Range: 290-310C
- Bed Temp Range: 25-50 C (Do not exceed 50C)
- Speeds: 40-50 mm/s
- Fan/Cooling: OFF
- Retraction: --
- Layer Height Range: --
Drying Info:
80-100C for 10-48 hours (full reel=80 for 48 hrs; low reel=100C for 10hrs)
Annealing Info:
80-100C for 30min - 3hrs
(dependent on size and density of your model, smaller model=higher temps, shorter time; larger model=lower temp, longer time)
NOTES: https://polymaker.com/introducing-n600-series/
___________________________________________________________________________________

Material Name: PETG
Material Type: Polyethylene Terephthalate Glycol
Manufacturer: IC3D
SDS Link: http://devel.alephobjects.com/lulzbot/filament/ic3d/PETG/SDS/
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/ic3d/PETG/REPORT/
Material Basic Info
- Print Temp Range: 230-270 C
- Bed Temp Range: 60-75 C
- Speeds: 10-40 mm/s
- Fan/Cooling: ON but Low
- Retraction: --
- Layer Height Range: --
Drying Info: 65 C for more than 2 hours
NOTES: Dry this filament if it has been left out in open air for more than 1 week.
DUAL COMPATIBILITY NOTES:
Ninjaflex is a Compatible Material for PETG. (NOTE: Turn DOWN the cooling fan on the NINJAFLEX PROFILE)
___________________________________________________________________________________

Material Name: INOVA 1800
Material Type: Co-polyester INOVA 1800
Manufacturer: Chroma Strand Labs
SDS Link: http://devel.alephobjects.com/lulzbot/filament/chromastrand/SDS's/AM1800_msds.pdf
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/chromastrand/Inova/Testing_Docs/lulzbot_green_chromastrand_prima_testing_report.pdf
http://devel.alephobjects.com/lulzbot/filament/chromastrand/Inova/Testing_Docs/lulzbot_green_chromastrand_prima_testing_report.odt
Material Basic Info
- Bed Adhesion Needs: PEI + Gluestick
- Print Temp Range: 230-250 C
- Bed Temp Range: 60-80 C
- Speeds: 40 mm/s
- Fan/Cooling: ON
- Retraction: 1/10 mm/s
- Layer Height Range: 0.05-1.2 mm
Drying Info: 65 C (150F) for 6 Hours
https://www.eastman.com/Literature_Center/S/SPTRS3100.pdf
Annealing info: NONE.
___________________________________________________________________________________

Material Name: PLA
Material Type: Polylactic Acid
Manufacturer: IC3D
SDS Link: http://devel.alephobjects.com/lulzbot/filament/ic3d/SDS/IC3D%20SDS%20PLA%20V2W.pdf
REPORT Link: Unavailable
Material Basic Info
- Print Temp Range: 200-240 C
- Bed Temp Range: 45-60 C
- Speeds: --
- Fan/Cooling: ON
- Retraction: --
- Layer Height Range: --
Drying Info: 45 C for 4 hours
NOTES: None.
___________________________________________________________________________________

Material Name: PA6/66 - GF20
Material Type: Glass Filled Nylon
Manufacturer: Clariant
SDS Link: http://devel.alephobjects.com/lulzbot/filament/Filament_Tech/Filament_info/SDS%20&%20Assessments/Clariant/SDS-Checklist_Clariant_P6/(1)%201.75%20MM%20PA6_66-GF20%20BLACK%203D%20FILAMENT_MSDS-US_EN_V1.2.PDF
REPORT Link: http://devel.alephobjects.com/lulzbot/filament/Clariant/PA6-66_GF20/66GF20-black.odt
Material Basic Info
- Print Temp Range: 240C - 260C
- Bed Temp Range: Ideally 80C
- Speeds: 20 - 50mm/s
- Fan/Cooling: Off to Low
- Retraction: --
- Layer Height Range: --
Drying Info:
160F - 180F for 6 - 8 hours
___________________________________________________________________________________

Material Name: AquaSys 120
Material Type: Water Soluble Polymeric Composite Material
Manufacturer: Infinite Material Solutions
SDS Link: https://infinitematerialsolutions.com/wp-content/uploads/2019/06/AquaSys120-SDS_190606.pdf
REPORT Link:
Material Basic Info
- Build Plate Adhesion:
- Print Temp Range:
- Bed Temp Range:
- Speeds:
- Fan/Cooling:
- Retraction:
- Layer Height Range:
Drying Info:
NOTES: